## Slide 1: Composites

## Slide 2: Composite Materials
Modern applications require materials with unusual combinations of properties
These properties might even be contradictory
Nature gives good examples: Wood (strong and flexible cellulose fibers embedded in stiff lignin) or bone (strong and soft collagen combined with hard and brittle apatite)
What kind of geometrical arrangements are generally possible?

## Slide 3: Main divisions of Composite Materials
Composites
Particle-reinforced
Fiber-reinforced
Structural
Large particles
or
Dispersion strengthened
Continuous (aligned)
or
Discontinuous
(short)
Laminates
or
Sandwich panels

## Slide 4: What geometrical information do we need?
In order to describe the dispersed phase in the matrix the following terms are needed
  Concentration
  Size
  Shape
  Distribution
  Orientation

## Slide 5: Particle reinforced composites
Large particle composite
Main goal here is an improvement of mechanical properties
Rule of mixture for elastic modulus
Upper bound Lower bound
  Polymers with fillers
  Concrete
Dispersion strengthened composites
Think tempered martensite

## Slide 6: Fiber reinforced composites
Fiber reinforced composite materials are the technologically most important form of composite materials
Typical examples are
  Glass fiber reinforced polymers
  Carbon fiber reinforced polymers
The performance of such fiber reinforced composites – if everything else (fiber length, orientation etc.) is taken care of – critically depend on the interfacial bonding between fiber and matrix
This leads to a number of strategies to improve this bonding
  Plasma activation
  Chemical functionalization

## Slide 7: Layered composites
  Laminar composites and sandwich panels are the standard macroscopic technologically exploited forms of “layered” composite systems
  Coating technology allows to create relative complex layered composite structures with relative ease
  Here structures range from
  MBE superlattices to “standard” multi-layers
  However, these layered systems should not be confused with functional layered systems
  Example: Quest for ultimate technological hardness

## Slide 8
Materials
Degradation

## Slide 9: Materials Degradation
fatigue
fracture
mechanical
aqueous corrosion
high-temperature corrosion
chemically
abrasion
wear
tribological

## Slide 10: Electrochemical Corrosion
approx. 5% of a nations income is spent on corrosion
rust, HT corrosion..
oxidation reactions – metal gives up electrons
M Mn++ne-
anodic reaction
reduction reactions – species accepts electrons
Mn++ne- M
2H++2e- H2
cathodic reaction
electrochemical reaction: two half reactions
e.g. Zn=>Zn2++2e- / 2H++ 2e-=>H2(gas)
galvanic couple: Fe2++Zn=>Fe+Zn2+: potential: 0.323V
but: Cu2++Fe=>Cu+Fe2+: potential: 0.780V
corroding
anode
cathode

## Slide 11: Standard Hydrogen Reference Half-Cell
hydrogen gas
1M solution of H+ ions saturated with H2 gas at 25°C/1atm (mole/1000cm³)
Pt surface:
H2 “oxidation“ anodic reaction
H+ “reduction“ cathodic reaction
electromotive force series
susceptibility to corrosion

## Slide 12: Iron Corrosion - Rust Formation
rust
rust
(1) Fe+1/2 O2+H2O=>Fe2++2OH-=>Fe(OH)2
(2) 2Fe(OH)2+1/2O2+H2O=>2Fe(OH)3
RUST
cathodic(+e-)
anodic (-e-)

## Slide 13: Forms of Corrosion
uniform attack
over the entire surface (steel components)
-predictable
local corrosion /intercrystalline corrosion – pitting/crecive corrosion
little material loss
-initiated by localized surface defect
-stainless steels are prone to pitting
-concentration differences in electrolyte
stress corrosion / erosion corrosion
crack growth enhanced by corrosion
-wear + corrosion -> protection becomes ineffective
.....

## Slide 14: Corrosion Protection
galvanic protection – Zn coating
cathodic protection (sacrificial anode)
coatings/inhibitors (paint, enamel..)
corrosion.protection-oriented design

## Slide 15: High Temperature Corrosion
M+1/2O2=>MO
>500°C
rate is determined by diffusion
through scale
metal
Me
O
O
O
O
MeO
2
2-
2+
m

non-porous and adherent scale:
parabolic rate law

t
²=kpt
linear:
=klint
(instead of  often the weight gain W is measured)

## Slide 16: Materials Selection
1 analysis of the application
-functional - structural
-loading conditions
-environment (T,atmosphere)
-safety requirements
-service life
-recycling
-cost
-design
-one ore more parts
-engineering design (FEM)
valves, e.g. exhaust valve

## Slide 17: Materials Selection
2 materials preselection
-metal (steel, Aluminum..)
-polymer
-ceramic
-composite
-new material development
fulfillment of the loading criteria
cost/availability
manufacturing
joining
recycling
3 materials modification
-heat treatment
-coating (corrosion protection,
(wear resistance...)

## Slide 18: Materials Selection
4 materials/component testing
-mechanical properties
-corrosion resistance
-prototype – testing under near
service conditions
5 design modifications
e.g. Volkswagen 1l car:
Mg frame +
C-fibre reinforced epoxy