## Slide 1: Hypoeutectoid Steels (CC<0.76%) ( hypereutectoid)
dark
pearlite:
lamellae
of Fe3C and
ferrite
light
ferrite
Ck45 Cc=0.45%

## Slide 2: Hypoeutectoid Steels (CC<0.76%) ( hypereutectoid)
dark
pearlite:
light
 ferrite
Ck15 Cc=0.15%

## Slide 3: Hypo-Eutectoid Transformation
Austenite
two-phase regime:
precipitation of ferrite (cC<0.02%)
=> Austenite cC c0=>0.76
Ferrite + Pearlite

## Slide 4: Eutectoid Transformation: Pearlite
not instantaneously!! -> f(time)
T=727°C
diffusion: C into Fe3C lamellae

## Slide 5: Phase Transformation
diffusion: C into Fe3C lamellae
log time t
fraction of transformation y
nucleation
(e.g. at phase/grain
boundaries)
growth
(volume of parent
phase disappears)
y=1-exp (-ktn)
kinetics:
(Avrami equation)
r=A exp (-Q/RT)
Arrhenius relationship: thermally activated processes
rate r:
r=1/t0.5

## Slide 6: Pearlite Formation - Isothermal Transformation
fraction of transformation y
time [s]
temperature [°C]
time [s]
equilibrium
according to
Fe-C phase diagram
(even normal cooling:
10-20K below equlilibrium)
rapid cooling to 675°C
isothermal pearlite
formation
isothermal transformation diagram /
time temperature transformation: TTT plot
Austenite
Pearlite

## Slide 7: Alteration in Microstructure continuous cooling transformation (CCT)
coarse pearlite
slow cooling
fine pearlite
fast cooling
equilibrium:
lower T => shorter diffusion paths!
Austenite
Pearlite

## Slide 8: Bainite Formation
pearlite
bainite
pearlite formation:
increasing thermodynamic driving force
faster reaction
coarse => fine pearlite
bainite formation:
lower T: decreasing C diffusivity
very fine Fe3C needles in  ferrite

## Slide 9: Martensite Formation
pearlite
bainite
very fast cooling to RT
(no intersection with
transformation “ nose“)
C diffusion becomes extremely
slow -> negligible!!
bcc  + Fe3C
fcc 
thermodynamic driving force for
fcc=> bcc transformation increases
fcc turns in bct martensite lattice
almost instantaneously:
=> C remains dissolved interstitially

## Slide 10: Martensite Formation
bct unit cell of martensite
supersaturated solid solution
Fe
possible sites
for C atoms
c
a
c>a
martensite plates / austenite
=> high strength
=> brittle

## Slide 11: Heat Treatment – Mechanical Properties
Normalizing (Austenite)
slow cooling:
hypo-eutectoid: -ferrite+pearlite
hyper-eutectoid: pearlite + Fe3C
moderate cooling:
bainite
fast cooling:
martensite
reheat (250°C-600°C)
tempered martensite

## Slide 12: Mechanical Properties
100
700
Brinell
hardness (strength)
composition [%C]
tempered
martensite
ductility [%RA]
0
Fe3C precipitates
brittle (%RA HB )
adherent phase boundaries
=>constraint for  deformation
coarse pearlite
fine pearlite
spheroidite
(approx. 700°C
annealed pearlite)
1%
martensite
martensite
=>no ductility
=>C blocks dislocation
motion

## Slide 13: Tempered Martensite
normalized (austenite)
water-quenched (=> martensite, brittle+internal stresses)
reheating (650°C)
=>C diffusion is possible
=>fine-dispersed Fe3C precipitates

## Slide 14: Tempered Martensite
good combination
of
1 strength
and
2 ductility

## Slide 15: Strengthening Mechanisms in Metals
1 grain size reduction
grain boundary acts as barrier to dislocation motion
due to: direction change (misorientation)
dicontinuity of slip planes
=> Hall-Petch relationship: Y=0+kYd-1/2
how can the grain size be modified?
control of solidification rate (fast)
avoid grain growth (high temperatures)
plastic deformation + heat treatment (recovery + recrystallization)
2 Strain Hardening/Work Hardening
increase in dislocation density

## Slide 16: Recovery and Recrystallization
e.g. rolling:
stored internal strain
energy
heat treatment:
rearrangement of
dislocations nucleation
and growth of new grains
in-situ recrystallization in the SEM

## Slide 17: Recrystallization Temperature
= new grain formation (recrystallization) finished after 1h
depends on: degree of cold work
in-situ recrystallization during hot working (e.g. hot rolling)
annealing temperature
UTS
[MPa]
grain
size
[mm]
Ductility
percent cold work
recrystallization temperature

## Slide 18: Strengthening Mechanisms in Metals
3 solid solution strengthening
by alloying elements
lattice strains  restrict dislocation motion
4 precipitation hardening
incoherent precipitates: e.g. carbides in steels,
=barriers to dislocation motion/constraints
coherent precipitates: e.g. ´phase in Ni-base superalloys
or ´´ phase in Al-Cu alloys
=cutting – barrier effect by disrupting the order/new interfaces

## Slide 19: Precipitation Hardening
cutting coherent ´particles (Ni3Al) in Ni-base superalloys
dislocation
slip plane
generation of disorder