## Slide 1
Structural Materials

## Slide 2: The Iron-Carbon Phase Diagram
eutectic system
eutectoid subsystem
peritectic subsystem
bcc  ferrite
fcc  austenite
bcc  ferrite
cementite Fe3C
Steel
Cast Iron

## Slide 3: Ferrous Alloys
Steels
(< 2%C – technically <1%C)
Cast Irons
(> 2%C – technically 2.5-4%C)
low alloy
high alloy
low C
(<0.25%C)
medium C
high C
plain
high
strength
plain
heat
treatable
plain
tool
stainless
heat-resistant
=> economical production process (natural resources, extraction, alloying, fabrication)
=> extremely versatile – wide range of physical/mechanical properties possible

## Slide 4: Low-Carbon Steels
plain
greatest quantity
cC<0.25% ferritic-pearlitic, Y275MPa
strengthening only by cold work
ductile=> machinable, weldable,
inexpensive
applications:
automobile bodies
structural shapes
(e.g. construction beams)
high-strength low-alloy
calloying elements<10%, Y480MPa
more critical structures
(bolted, low temperatures...)

## Slide 5: Medium (High) Carbon Steels
cC=0.25...0.6% (, suitable for heat treatment hardening, Y400-2000MPa
strengthening by
-austenitizing (normalizing)
-quenching (often surface)
-tempering
(by addition of Cr, Ni, Mo)
applications:
railway wheels, gears..
high C steels:
cutting tools, springs, wire..
soft core –
hard/wear resistant surface

## Slide 6: High-Alloy Steels
cCr>11% => corrosion resistant
1 martensitic
cutlery (surgery knifes)...
2 austenitic (fcc at RT by adding Ni
chemical, food processing
construction...
3 ferritic
(very) high temperatures (Cr up to 25%), automotive exhaust
systems catalytic converter...
2-3 strengthening only by cold work
or precipitation hardening

## Slide 7: Cast Irons
cC>2.14%, typical 3...4.5%
low liquidus betw. 1150...1300°C
=> fluidity at casting temperature
stable Fe – C system!!
gray cast iron (slow cool):
ferrite + graphite flakes
weak/brittle
damping properties
wear resistant
low casting shrinkage
cheap !!
stronger
and
ductile
+ Mg, Ce (slow cool):
ferrite + graphite nodules

## Slide 8: Cast Irons
fast cool:
white cast iron
cementite + pearlite
brittle/hard
heat treatment => malleable:
Fe3C decomposition:
graphite + ferrite (pearlite)

## Slide 9: Non-Ferrous Alloys
disadvantages steel:
-high density (7.85g/cm3)
-low conductivity
-poor corrosion resistance (low-alloy steels)
-lack of “ special“ properties
Al alloys (1/3 density, corrosion resistant, conductive)
Mg alloys (lowest density)
Ti alloys (low density, high strength, corrosion resistance)
Ni alloys (corrosion resistance also at high temperatures)
Cu alloys (conductive, corrosion resistance)
refractory metals (Nb, Mo, W, Ta – very high Tm (W: 3410°C)
noble metals (Au, Pd, Pt..functional materials: catalysts)
others (Pb, Zn, Sn, functional materials, corrosion protection)

## Slide 10: Aluminum Alloys
low density (2.7g/cm³) fcc
Tm=660°C (technical limit!!), E=70GPa
corrosion resistant/conductive/formable
heat-tretable: e.g. MgZn2 particles
but limited weldability
applications:
automotive bodies/aircraft structures/
furniture/wheels etc.

## Slide 11: Magnesium Alloys
very low density (1.7g/cm³) hcp
Tm=651°C, E=45GPa
susceptible to corrosion
mostly cast
(e.g. AZ91, Mg-Li alloys)
applications:
e.g. gear boxes, steering wheels, hand-held devices

## Slide 12: Titanium Alloys
low density (4.5g/cm³) a hcp above 880°C  bcc
Tm=1670°C, E=107GPa
corrosion resistant (up to approx. 600°C)/
biocompatible
heat treatable -> -two phase microstructure
applications:
 Ti-6Al-4V: implants, structural airframe
components
near Ti-8Al-1Mo: compressor disks
 Ti-10V-2Fe-3Al: high strength applications: e.g. springs,
landing gear, rotor heads

## Slide 13: Copper Alloys
high density (8.2g/cm³) fcc
Tm=1083°C, E=130GPa
corrosion resistant, conductive
heat-treatable (high strength CuBe alloys, 1...2.5% Be)
brass (e.g. Cu-37%Zn)
bronze (e.g. Cu-30%Ni)
applications:
e.g. water pipes, roofs, electric/electronic devices/nuts/
propellers...

## Slide 14: Nickel-Alloys - Superalloys
high density (8.9g/cm³) fcc
Tm=1453°C, E=210GPa
corrosion resistant (up to very high temperatures)/ alloyable
based on Ni-20Cr-5Al: superalloys:
precipitation strengthened (-Ni3Al)
creep resistant
(also: Fe-based and Co-based superalloys)
applications:
petrochemical industry, heating elements,
energy production – gas turbines

## Slide 15: Metal Fabrication
Forming Operations
forging rolling
extrusion drawing
Casting
sand die
investment continuous
Miscellaneous
powder metallurgy welding

## Slide 16: Metal forming
forging
rolling
heat treatment: normalizing, hardening, recrystallization..
extrusion
drawing

## Slide 17: Heat treatment
Annealing
Process annealing
Stress relief
Annealing of ferrous alloys
normalizing
Full anneal
Spheroidizing
Hardenability
The Jominy End-Quench Test

## Slide 18: Reminder: Iron-Carbon Phase Diagram

## Slide 19: Alteration in Microstructure continuous cooling transformation (CCT)
equilibrium:
Austenite
Pearlite

## Slide 20: Precipitation Heat Treatment
fast cooling => supersaturation
Cu in solid solution
solution
heat tretament
aging

## Slide 21: Ceramics

## Slide 22: Ceramics
inorganic – non-metallic materials
china/dishes
cemente/concrete
functional ceramics
structural ceramics
structures depending on a) electrical charge
b) atomic radii (rC/rA)
ionic – covalent bonding of at least 2 atoms
(e.g. Al2O3: 63% ionic, SiC: 12% ionic)
+
cation
-
anion
electrons
stable – cations are in contact with surrounded anion

## Slide 23: Structure of Ceramics
coordination number 6 rC/rA:
coordination number 4 rC/rA:
coordination number 8 rC/rA:
e.g.: Al2O3:
Al3+: rC=0.053nm, O2-: rA=0.140nm

## Slide 24: AX Structures
e.g. NaCl
fcc anionic (Cl-) lattice
fcc cationic (Na+) lattice
two interpenetrating fcc lattices:
e.g. MgO, MnS, FeO
(coordination number 6)

## Slide 25: AmXp Structures
e.g. CaF2
rC/rA=0.8
coord. 8
center cube positions
only half-filled
(CsCl completely-filled)
AmBnXp Structures
e.g. BaTiO3