## Slide 1: Polymers
PA in PP matrix

## Slide 2: From Natural to Synthetic Polymers
natural: wood, rubber, cotton, wool, leather, silk etc.
CH4 (methane)
H
H
C
H
C2H4 (ethylene)
H
H
H
H
C
C
H
saturated
unsaturated
(double, triple bonds)
synthesis of small organic molecules, e.g. hydrocarbons

## Slide 3: Paraffin Family - Isomerism
CnH2n+2
e.g. C4H10 (butane)
H
H
H
H
C
C
H
H
H
H
C
C
H
H
C4H10 (isobutane)
H
H
H
C
C
H
H
C
H
H
H
C
H
H

## Slide 4: Polymer Macromolecules - Chains
C atoms chain backbone
C
C
C
C
C
C
C
mer: repeated units
monomers => polymers
H
H
e.g. ethylene C2H4
monomer
H
H
C
C
+R (initiator / catalyst species)
H
H
H
H
C
C
R
H
H
H
H
C
C
R
H
H
H
H
C
C
H
H
H
H
C
C
H
H
H
H
C
C
polymer

## Slide 5: Polymerization and Processing
monomers
active initiator
additives (filler,colorants..)
chain growth
termination (R-C-C-R)
extrusion
injection molding (very fast)
pressure
temperature
3D structure

## Slide 6: Monomers => Polymers
F
F
F
F
C
C
polytretrafluorethylene
PTFE
polyvinylchloride
PVC
H
H
H
Cl
C
C
H
H
H
CH3
C
C
polypropylene
PP
H
CH3
H
CH3
C
C
H
H
H
H
C
C
O
polyethylene terephtalate
PET
aromatic
ring

## Slide 7: Characteristics: Molecular Weight
chain length  molecular weight M
100g/mole – short chains: liquid state
1000g/mole – waxy solids
>10000g/mole – high polymers: solids
degree of polymerization n
(average number of mer units in chain)
mer molecule weight (homopolymercopolymer)

## Slide 8: Characteristics: Molecular Weight
polymerization:
polymer chains of different length – molecular weight
number average molecular weight:
number fraction
(how many polymers of Mi)
weight fraction
(weight of polymers of Mi)
weight average molecular weight:

## Slide 9: Average Molecular Weight

## Slide 10: Characteristics: Shape
C backbone => 109° angles:
C
C
C
intertwining/coils

## Slide 11: Characteristics: Structure
linear polymers
(like spaghettis, e.g. PE,PVC,PS)
branched polymers
(side reactions)
crosslinked polymers
(by addtl. molecules, e.g. epoxies)

## Slide 12: Characteristics: Structure
network polymers
(trifunctional mer units, e.g. epoxies)

## Slide 13: Molecular Configurations
H
H
H
R
C
C
side groups (e.g. Cl, CH3) => regularity – symmetry=> properties
stereoisomerism
(isotactic, syndiotactic, atactic)
H
H
H
R
C
C
H
H
H
R
C
C
head to tail
H
H
H
R
C
C
H
H
H
R
C
C
head to head
geometrical isomerism
e.g. polyisoprene
cis: natural rubber
H
CH3
H
C
C
H
H
C
C
H
cis
H
CH3
H
C
C
H
H
C
C
H
trans

## Slide 14: Thermoplastic - Thermosetting
when heating
crosslinked polymers
degradation
soften
liquefy
(diminishing secondary
bonding forces => fabrication)
PTFE (e.g. teflon, chemically inert,
low friction, T<260°C)
PA (e.g. nylon) PE/PP (bottles, toys, containers)
Acrylics (PMMA polymethyl methacrylate,
transparent)
Vinyls (floor covering, records)
epoxies (adhesives)
polyester (fiberglas,
helmets, auto body comp.)

## Slide 15: Improving Properties
homopolymers => copolymers
random
alternating
block
graft
e.g. synthetic rubbers
automobile tires SBR
gasoline hoses NBR
defects
-impurities
-vacancies
mostly at chain ends
diffusion properties
=> interstitial mechanism
e.g. bottles, membranes

## Slide 16: Crystalline Polymers
packing of molecular chains
=> usually not complete
orthorombic PE
unit cell
depends on
-cooling rate (slow)
-chain configuration (simple)

## Slide 17: Mechanical Properties of Polymers
elastomers
partial uncoiling
decreasing entropy
e.g. polyisopropene (NR)
acrylonitrile butadiene
copolymer (NBR)
Y (necking – chain ordering)
increasing temperature/
decreasing strain rate
(U)TS – max. 100MPa, E=7...4000MPa
brittle (thermosetting)
ductile(depends on T, d/dt)
=> crazing
fracture:

## Slide 18: Mechanical Properties of Polymers
mechanical load step
elastic
viscoelastic
viscous
depends on -strain rate
-temperature
-structure

## Slide 19: Mechanical Properties of Polymers
load relaxation (=const)
relaxation modulus
Er(t)=(t)/0
log time
t1
temperature (°C)
viscoelastic
glassy
(brittle)
Er(t1)
glass transition temperature